HTI Filtration, Inc.

TECHNICAL BULLETIN

Bulletin 12-12-98-1                   					       		Date: 12-12-98

RE: Model 810-020 Hydra-Tech Hydraulics Filtration Unit Water Absorption Test

Overview:  The Hydra-Supreme 810-020 filtration system will swell as it absorbs water and debris from the host machines oil supply causing the pressure to rise and the flow to gradually diminish. To obtain maximum filter life it is desirable to operate the filter until the pressure increase 30 PSI or the flow drops off to .25 GPM. The red strobe light will typically activate at 55-60 PSI indicating that the filter has reached full capacity.  Continued use of the saturated filter element may allow water and debris to build up to potentially damaging levels.

.55

F

L      .50        				Water Absorption and Flow Correlation

O

W     .45

in      .40

G      .25

P							700 ML WATER

M      .20

.15

0.0

0	100	200	300	400	500	600	700   800 	                			WATER  IN ML

70

P

R	60							     65 PSI

E

S	50

S							700 ML TOTAL

U	40				Water Absorption and Pressure Correlation

R

E	30

28 PSI

IN	20

P	10

S

I	0

0	100	200	300	400	500	600	700   800 		                						WATER  IN ML

810-020 water absorption test                                             All tests run using 750 SUS oil @ 100 Fo